Optical Encoder Discs

GLASS - Highest performance, best resolution, critical applications

Maximum OD:                  300mm
Thickness:                    0.3mm–6.3mm
Minimum feature size:           3μm
Operating Mode:               Transmissive / Reflective
Material:                      Sodalime, Borosilicate, Quartz
Pattern metallization:         High/low reflective coating, chrome, gold, and aluminum

PET (MYLAR) - Low-cost alternative, easy installation

Maximum OD:             600mm
Thickness:               0.18mm (Transmissive) / 0.3mm (Reflective)
Minimum feature size:      10μm
Operating Mode:         Transmissive / Reflective
Material:                Photographic film, composite PET, acrylic, and PSA backing

ALUMINUM - Ideal for extreme environmental conditions

Maximum OD:                   250mm
Thickness:                       0.5mm
Minimum feature size:            10μm
Operating Mode:                  Reflective
Material:                         1100 Aluminum alloy