| Item | Transmissive Glass Scale | Reflective Glass Scale |
| --- | --- | --- |
| METALLIZATION — 99.999% CHROME |  |  |
| Optical Density |  |  |
| Minimum Feature Size |  | 5um |
| Bar/Window Ratio (50/50) | +/- 2um | +/- 2um |
| Maximum Length | 165 mm | 165 mm |
| Pattern to Scale Outline (scribe and break) | +/- 165um | +/- 165um |
| Pattern to Scale Outline (saw) | +/- 5um | +/- 5um |
| Edge Chip Specification | Maximum .010” (250 um) / Special to 20um | Maximum .010” (250 um) / Special to 20um |
| Flatness Over Entire Substrate | 15um, Special to 5um | 15um, Special to 5um |
| Parallelism | .001” over 4” | .001” over 4” |
| SUBSTRATE - SODALIME GLASS |  |  |
| Density | 1-5+ | 1-5+ |
| 2.8d or 1000 Angstroms | 2.8d or 1000 angstroms | 2.8d or 1000 angstroms |
| Reflective Coating | High or low reflective coating | High or low reflective coating |
| Thickness | .012” - .250” (.30-6.35 mm) | .012” - .250” (.30-6.35 mm) |
| SODA LIME GLASS SUBSTRATE PROPERTIES |  |  |
| Refractive Index | 1.523 (435nm), 1.513 (645 nm) | 1.523 (435nm), 1.513 (645 nm) |
| Thermal Conductivity | 0.937 W.m/m²°C | 0.937 W.m/m²°C |
| Soda Lime TCE | (0/300 °C): 8.6 x 10⁻⁶/°C | (0/300 °C): 8.6 x 10⁻⁶/°C |
| Annealing Point | 546°C / 1015°F | 546°C / 1015°F |
| Strain Point | 514°C / 957°F | 514°C / 957°F |
| Softening Point | 726°C / 1340°F | 726°C / 1340°F |
| Substrate Density | 2.44 g/cm³ @ 20°C / 68°F | 2.44 g/cm³ @ 20°C / 68°F |
| Modulus of Elasticity (Young's) | 7.2 x 10¹⁰ Pa | 7.2 x 10¹⁰ Pa |
| Modulus of Rigidity (Shear) | 3.0 x 10¹⁰ Pa | 3.0 x 10¹⁰ Pa |
| Bulk Modulus | 4.3 x 10¹⁰ Pa | 4.3 x 10¹⁰ Pa |
| Poisson's Ratio | .22 | .22 |
| Density (at 20°C/68°F) | 2.44 g/cm³ | 2.44 g/cm³ |
| Hardness (Moh's Scale) | 6-7 | 6-7 |
| Knoop Hardness | 585 kg/mm² ± 20 | 585 kg/mm² ± 20 |
| Specific Gravity | 2.53 | 2.53 |
| Specific Heat | 0.21 | 0.21 |
| Specific Weight | 2,483 g/cm³ | 2,483 g/cm³ |