1.Applicable     Scope

This specification is suitable for Xian Photo reticle  optoelectronic Instrument Co.Ltd.

##### 2.Substrate       Specification

##### 2.1 Soda lime glass substrates

Surface:All plates polished on both sides。

| Type | Material | Dimension and Thickness(inch) | Flatness (μm) | Dimension(mm) |  | Thickness (mm) |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | min | max | min | max |
| 3004 | S | 3.0×3.0×0.06 | ≤5 | 75.4 | 76.2 | 0.90 | 1.05 |
| 3006 | S | 3.0×3.0×0.06 | ≤5 | 75.4 | 76.2 | 1.40 | 1.60 |
| 3006 | WC | 3.0×3.0×0.06 | ≤20 | 75.4 | 76.2 | 1.50 | 1.55 |
| 4004 | S | 4.0×4.0×0.04 | ≤5 | 100.8 | 101.6 | 0.90 | 1.05 |
| 4004 | WC | 4.0×4.0×0.04 | ≤20 | 100.95 | 101.45 | 0.97 | 1.03 |
| 4006 | S | 4.0×4.0×0.06 | ≤5 | 100.8 | 101.6 | 1.40 | 1.55 |
| 4006 | WC | 4.0×4.0×0.06 | ≤20 | 100.8 | 101.6 | 1.45 | 1.55 |
| 4007 | WC | 4.0×4.0×0.07 | ≤20 | 100.8 | 101.6 | 1.75 | 1.85 |
| 4008 | S | 4.0×4.0×0.08 | ≤5 | 100.8 | 101.6 | 1.95 | 2.05 |
| 4008 | WC | 4.0×4.0×0.08 | ≤20 | 100.8 | 101.6 | 2.00 | 2.05 |
| 4009 | S | 4.0×4.0×0.09 | ≤5 | 100.8 | 101.6 | 2.20 | 2.40 |
| 4009 | WC | 4.0×4.0×0.09 | ≤5 | 100.8 | 101.6 | 2.30 | 2.40 |
| 4010 | S | 4.0×4.0×0.10 | ≤5 | 100.8 | 101.6 | 2.44 | 2.64 |
| 4010 | WC | 4.0×4.0×0.10 | ≤20 | 100.8 | 101.6 | 2.50 | 2.60 |
| 4012 | S | 4.0×4.0×0.12 | ≤5 | 100.8 | 101.6 | 2.95 | 3.05 |
| 4012 | WC | 4.0×4.0×0.12 | ≤20 | 100.8 | 101.6 | 2.95 | 3.00 |
| 4014 | WC | 4.0×4.0×0.14 | ≤20 | 100.8 | 101.6 | 3.40 | 3.55 |
| 4016 | WC | 4.0×4.0×0.16 | ≤20 | 100.8 | 101.6 | 4.00 | 4.05 |
| 4018 | WC | 4.0×4.0×0.18 | ≤20 | 100.8 | 101.6 | 4.50 | 4.55 |
| 4020 | WC | 4.0×4.0×0.20 | ≤20 | 101.2 | 101.4 | 4.90 | 5.00 |
| 4026 | WC | 4.0×4.0×0.26 | ≤20 | 101.2 | 101.4 | 6.45 | 6.55 |
| 5002 | S | 5.0×5.0×0.02 | ≤20 | 126.2 | 127.0 | 0.45 | 0.55 |
| 5002 | WC | 5.0×5.0×0.02 | ≤20 | 126.2 | 127.0 | 0.45 | 0.55 |
| 5004 | S | 5.0×5.0×0.04 | ≤20 | 126.2 | 127.0 | 0.95 | 1.05 |
| 5004 | WC | 5.0×5.0×0.04 | ≤20 | 126.2 | 127.0 | 0.95 | 1.05 |
| 5006 | WC | 5.0×5.0×0.06 | ≤20 | 126.2 | 127.0 | 1.45 | 1.55 |
| 5008 | WC | 5.0×5.0×0.08 | ≤20 | 126.2 | 127.0 | 2.00 | 2.05 |
| 5009 | S | 5.0×5.0×0.09 | ≤8 | 126.2 | 127.0 | 2.20 | 2.40 |

| 5010 | WC | 5.0×5.0×0.10 | ≤20 | 126.2 | 127.0 | 2.45 | 2.55 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 5012 | WC | 5.0×5.0×0.12 | ≤20 | 126.2 | 127.0 | 2.95 | 3.05 |
| 5014 | WC | 5.0×5.0×0.14 | ≤20 | 126.2 | 127.0 | 3.45 | 3.55 |
| 6009 | S | 6.0×6.0×0.09 | ≤10 | 151.6 | 152.4 | 2.20 | 2.40 |
| 6009 | WC | 6.0×6.0×0.09 | ≤20 | 151.75 | 152.25 | 2.30 | 2.40 |
| 6012 | S | 6.0×6.0×0.12 | ≤10 | 151.6 | 152.4 | 2.95 | 3.15 |
| 6016 | WC | 6.0×6.0×0.16 | ≤20 | 151.6 | 152.4 | 4.00 | 4.10 |
| 6023 | S | 6.0×6.0×0.23 | ≤10 | 151.6 | 152.4 | 5.75 | 5.95 |
| 6025 | S | 6.0×6.0×0.25 | ≤10 | 151.6 | 152.4 | 6.25 | 6.45 |
| 7009 | S | 7.0×7.0×0.09 | ≤15 | 177.0 | 177.8 | 2.20 | 2.40 |
| 7012 | S | 7.0×7.0×0.12 | ≤15 | 177.0 | 177.8 | 2.95 | 3.15 |
| 7012 | WC | 7.0×7.0×0.12 | ≤30 | 177.0 | 177.8 | 2.95 | 3.15 |
| 8012 | S | 8.0×8.0×0.12 | ≤15 | 202.4 | 203.2 | 2.95 | 3.15 |

S:Soda-lime;WC:White Crown

##### 2.2 Squareness  ：90°±5'

2.3 Edges:Chamfering 45°is required forall substrates.

Edge  profile:Beveling.

##### 2.4   Corner

>1 6       0.40  0.80   2.00    3.00

| T | B |  | R |  |
| --- | --- | --- | --- | --- |
| (mm) | min | max | min | max |
| ≤1.6 | 0.20 | 0.50 | 2.00 | 3.00 |
| . |  |  |  |  |

##### 2.5 Glass Appearances

| No. | Defect | Specification |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Surface and Substrate's inner |  |  | Inspection area |
| 1 | Broken,Chip | Not | allowed | >2mm | Effective Area |
| 2 | Bubble,Indusion | Not | allowed | >5μm |  |
| 3 | Pit | Not | allowed | >5μm |  |
| 4 | Scratch | Not | allowed | >5μm*1mm |  |

##### 2.6   Effective   area

D=L-25.4/2

Inspect  method:Under  theillumination  of  120,000  Lux  of  Halogen  lamp   15cm away check  by  naked eyes。

##### 3.Chrome Film Specification

| Item | Film |  | Optical density |  | Reflectivity |  | Wet etching time | Chemical Resistance |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Instrument | AlphasteplQ IKLA-Tencor |  | D200 II/Macbeth |  | U-3010VVarian |  |  |  |  |
| Condition | Type | Thickness |  | Wave length |  | Wave length | Manual | conc. 98%H₂SO @120°℃ | SPM @75℃ |
| Type-1 | LRC | 1000±B0 A | 3.1±0. | 450nm | 11±2% | 436nm | 43-53 sec | >120min | >120min |
| Type-2 | LRC | 1250±100A | 4.0±02 | 450nm | 11±2% | 436nm | 50-60 sec | >120min | >120min |
| Type-3 | BCB | 2000±200 A | 5.0±0. | 450nm | S7% | 600±50nm | 》70 sec | >60min | >60min |
| Type-4 | LRC | 2000±200 A | 5.0±0. | 450nm | 11±2% | 438nm | >70 sec | >120min | >120min |
| Typ-5 | HRC | 1000±100 A | 3.1±0. | 550nm | 245% | 438nm | 43-53 sec | >120min | >120min |
| Type-6 | BCB | 2500±200 A | 5.0±0. | 500nm | S7% | 600±50nm | >70 sec | >60min | >60min |
| Type-7 | LRC | 1250±100 A | 3.1±0. | 550mm | 11±2% | 436nm | 50-60 sec | >120min | >120min |
| Type-8 | HRC | 2000±200 A | 5.0±0. | 550nm | 245% | 436nm | >70 sec | >120min | >120min |

LRC:low reflective chrome:HRC:highreflective chrome:BCB:blue-chrome-blue Undercut    rate    except    Type    BCB(both    sides):<0.07μm/10s

3.1   Wet   etching   conditions

Dipping:thermostat  20℃±0.1℃ with  stirring

Etchant:CericAmmonium     Nitrate       200g

Acetic Acid(glacial)             35ml

DI Water

Total:                                  1000ml

3.2   Frequency   of   measurement    and   method

The   optical   properties:one    dummy/one   lot.

3.3 pinhole:

| Grade | Chrome fim |  |
| --- | --- | --- |
|  | Size | Specification |
| High Grade | <2μm | No Limit |
|  | 2μm-5μm | ≤0.3pcs/inch2 |
|  | >5μm | None |
| Standard Grade | >2μm | ≤0.5pcsinch2 |
|  | >5μm | None |
| Blue-Chrome-Blue | >5μm | S0.5pcsinch2 |
|  | >10μm | None |

##### 3.3.1 Frequency oflnspect

Full inspection

4.Photoresist                  Film

##### 4.1 Photoresist type

| Grade | Resist |  |  | Area shape |
| --- | --- | --- | --- | --- |
|  | Resist type | Thickness | unifomity |  |
| High Grade | AZ 1500 | 5000A | ±1% | Square/Cirdle |
| Standard Grade | AZ 1500 | 5000A | ±2% | Square/Cirdle |
| High Grade | IP 3500 | 4600A | ±1% | Circle |
| Standard Grade | AZ TFP650 | 7000A | ±3% | Square/Cirdle |
| Standard Grade | AZ TFP650 | 10000A | ±3% | Square/Cirdle |

##### 4.1.1 Frequency of measurement and method

The thickness &uniformity :one dummy/one lot。

4.2   Inspect   method   of  resist.

Full inspection.Under the yellow illumination of 120,000 Lux of Halogen lamp 15

cm away check by naked eyes.

4.3    Recommend     developing.

AZ 300MIF(2.38%):   23C/60sec

##### 5.Package

Products are packed in a black box which packed in aluminium foil paper and PE film under vacuum package,for insulating from contaminations and light.

##### 6.Product      labeling

Labels will be attached on each black box and contents as follows:

Product  Model

Quantity  report

Lot ID

##### 7.Others

7.1 Further detail or technical disagreement of the above specification

statement shall be settled in a formal meeting 。Meeting agreement should be included in the specification immediately。

##### 77.2 This product quality assurance is valid for three months for photoresist

(CD  and  defect  )。

Storage environment:temperature 20±5℃,humidity is 45±5%。

77.3 Official notices should announce the date of change and items of change    before updating the manufacturing engineering or quality control process。

7.4 Quality problems shall be settled based on results of inspector 。Problem settlement should be achieved by consulting with customer cooperation to